## Slide 1
Spectral Signatures and Spatial Coherence of “Bound” and “Unbound” Polarons in P3HT Films: Theory vs Experiment
Raja Ghosh
Supervisor: Prof. Frank Spano
Temple University
1

## Slide 2
Interchain
Interactions
Background
P3HT Chain
Single Chain Polaron
Interchain Polaron
2
Osterbacka et. al. Science 2000

## Slide 3
F4TCNQ doped P3HT Films
B
A
Undoped P3HT Films
B
A
Kahmann, et. al, J. Mater. Chem. C 6, 6008 (2018).
Scholes, et al. Adv. Funct. Mater. 2017.
With Increasing order and crystallinity in the sample,
Peak B and A redshifts.
Peak A increases in intensity
Background
Increasing Order
Increasing Order
What is the nature and origin of the two peaks?
3

## Slide 4
Modelling Polymer Aggregates with Vibronic Coupling: Holstein Hamiltonian
P3HT backbone
P3HT stack
tintrachain
tinterchain
Intrachain
Interchain
What are the mid- IR Spectral Signatures of Delocalized Polarons?
Over what distances are holes/Polarons delocalized along the backbone in a P3HT chain?
and
How many Chains?
Shine light
+
+
0.35 – 0.40 nm
Theory
4
R. Ghosh, C. M. Pochas, F. C. Spano, J. Phys. Chem. C 2016, 120, 11394.
Charge delocalization
Vibronic coupling

## Slide 5
Developed a relation between Oscillator strength and Coherence function:
The 2D hole coherence function is given by :
Coherence is promoted by strong electronic coupling and hindered by disorder and vibrational coupling
Polaron Coherence and Spectral line shape
Theory
5
R. Ghosh, C. M. Pochas, F. C. Spano, J. Phys. Chem. C 2016, 120, 11394.

## Slide 6
Site disorder, s = 0.2 eV
Site disorder, s = 0.4 eV
Energy
Position along the chain
+
Nintra = 5.23 (1.7 nm)
Ninter = 5.15 (1.66 nm)
Ncoh = 28 (2.8 nm2)
Nintra = 4.28 (1.31 nm)
Ninter = 3.66 (1.064 nm)
Ncoh = 17.70 (1.4 nm2)
Nintra = 2.76 (0.704 nm)
Ninter = 2.10 (0.44 nm)
Ncoh = 7.08 (0.31 nm2)
tintrachain
No disorder, Ideal Polymer
+
+
Dm,n chosen randomly from
a Gaussian distribution of width s
Localized hole
Polaron Coherence and Spectral line shape
Delocalized hole
6

## Slide 7
Undoped P3HT Films: Comparison to Experiment
(Electrically Generated holes- Charge-Modulation Spectroscopy)
Nintra = 5.23 (1.7 nm)
Ninter = 5.00 (1.6 nm)
Ncoh = 28 (2.72 nm2)
Nintra = 5.12 (1.65 nm)
Ninter = 2.14 (0.456 nm)
Ncoh = 12.44 (0.75 nm2)
A.R Chew, R. Ghosh, V. Pakhnyuk, J. Onorato, E.C. Davidon, R.A. Segalman, C.K. Luscombe, F.C Spano and A. Salleo, Unraveling the Effect of Conformational and Electronic Disorder in the Charge Transport Processes of Semiconducting Polymers, Adv. Funct. Mater. 2018, doi.org/10.1002/adfm.201804142
7
Take Home message
Increase in mobility below 12.6 kg/mol is due to progressively greater interchain order.
Increase in mobility above 12 kg/mol is due to increased crystalline connectivity via tie chains.

## Slide 8
+
Modelling Doped Polymer Chains: F4TCNQ doped P3HT films
Point charge
Coulomb Interaction between hole and anion
8

## Slide 9
Origin and nature of Polaron Peaks A and B
P3HT Chain having 10 thiophene units
Energy
danion
+
+
Position along the chain
Coulomb Interaction isolates 2 polaron levels
I
II
tintrachain
VI
I and II are in resonance and electronically coupled by the hole transfer integral
0.2 nm
0.2 nm
9

## Slide 10
2tintrachain
Origin of Polaron Peaks: Herzberg-Teller Coupling
I
II
tintrachain
(Peak B)
(Peak A)
No vibronic coupling, disorder
Herzberg Teller Coupling
Treat vibronic coupling, disorder pertubatively
Symmetric State
AntiSymmetric State
10

## Slide 11
+
danion
+
danion
+
danion
+
danion
IR Spectrum vs. Anion – Chain Distance
Single P3HT Chain
DisorderedP3HT Chain having 10 thiophene units
+
danion
0.2 nm
0.4 nm
0.6 nm
0.8 nm
1.0 nm
+
Peak B red-shifts
Peak A increases in intensity
11

## Slide 12
Interchain Effects: p-stacks
+
Delocalized Polaron
Take Home message
Peak A has higher intensity than peak B.
Peak A has both intrachain and interchain component.
Bound Polaron
Take Home Message
Peak B has higher intensity than peak A
Peak A is mainly intrachain.
+
12
Ghosh et al., Spectral Signatures and Spatial Coherence of Bound and Unbound Polarons in P3HT Films: Theory Versus Experiment. J. Phys. Chem. C , 2018, 122, 18048

## Slide 13
F4TCNQ-Doped Films: Comparison to Experiment
Nintra = 4.04 (1.22 nm)
Ninter = 1.62 (0.25 nm)
Ncoh = 7.35 (0.302 nm2)
13
Ghosh et al., Spectral Signatures and Spatial Coherence of Bound and Unbound Polarons in P3HT Films: Theory Versus Experiment. J. Phys. Chem. C , 2018, 122, 18048

## Slide 14
Polarized P3HT measurements: Comparison to Experiment
Take Home Message
Peak A cannot be explained by conventional Polaron theory and has contributions from intrachain component too. Peak A arises due to Herzberg Teller Coupling mechanisms
Low energy polaron signatures contain valuable information about polaron coherence, charge mobility.
14
Manuscript under preparation, 2019
Are there really any mid-gap states?
Do we need to review the definition of Polaron?

## Slide 15
Future Work: Donor Acceptor Copolymers
D
A
D
A
D
A
D
A
Segregated p-stack
Mixed p-stack
15
Manuscript under preparation, 2019

## Slide 16
teams
Theory
Frank Spano
Student:
Raja Ghosh
Characterization
Prof. Alberto Salleo
Students:
Dr. Annabel Chew
Zhengrong Shang
Synthesis
Prof. Christine Luscombe
Students:
Jonathan Onorato
Viktoria Pakhnyuk
Acknowledgement
Theory
Synthesis
Theory
Characterization
Synthesis
Characterization
16

## Slide 17
Acknowledgement
Prof. Benjamin Schwartz (UCLA)
Prof. Martin Brinkmann (University of Strasbourg)
Dr. Nicholas Hestand (University of Chicago)
Dr. David Bialas
Chuwei Zhong
April Oleson
Mohammad Balooch Qarai
Funding
THANKS to
For No TA duties!!
17

## Slide 19
Background
Polarons (holes) in Semiconducting Polymers:
Conventional Interpretation
Single Chain Polaron
P1 and P2 are mid-gap/Polaron states
Osterbacka et. al. Science 2000
+
P3HT Chain

## Slide 20
Polarons (holes) in Semiconducting Polymers:
Conventional Interpretation
Interchain Polaron
Osterbacka et. al. Science 2000
+
Interchain Interactions
Background

## Slide 21
Undoped P3HT Films: Comparison to Experiment
(Electrically Generated holes- Charge-Modulation Spectroscopy)

## Slide 22
+
+
+

## Slide 23
Modelling Disordered Polymer Chains
+
+
+
Nintra = 5.23
Ninter = 5.15
Ncoh = 28
Dm,n chosen randomly from
a Gaussian distribution of width s
Nintra = 4.28
Ninter = 3.66
Ncoh = 17.70
Nintra = 2.76
Ninter = 2.10
Ncoh = 7.08
Energy Levels